U.S. CUSTOMS AND BORDER

PROTECTION LABORATORY METHODS

CBPL METHOD 29-08

ASTM D 2369

Standard Test Method for Volatile Content of Coatings

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

This method describes a procedure for the determination of the weight percent volatile content of solvent based and water-reducible coatings.  Test specimens are heated at 110 ±5 degrees Celsius for 60 minutes.

This method has application to the determination of the volatile content of solvent soluble polymers provided for in Chapter 29 of the Harmonized Tariff Schedule of the United States (HTSUS).

1.		REFERENCE

1.1		ASTM D 2369.  “Standard Test Method for Volatile Content of Coatings.”

END