U.S. CUSTOMS AND BORDER

PROTECTION LABORATORY METHODS

CBPL METHOD 38-07

ASTM D 3008

Standard Test Method for Resin Acids in

Rosin by Gas-Liquid Chromatography

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

This method covers the determination of the resin acids in tall oil, gum, or wood rosin after conversion to their methyl esters.  It uses a packed column gas chromatograph.  This method is applicable to Chapter 38, Subheading 3806.10, of the Harmonized Tariff Schedule of the United States (HTSUS).

1.		REFERENCE

1.1		ASTM D 3008.  “Standard Test Method for Resin Acids in Rosin by Gas-Liquid Chromatography.”

ASTM discontinued this method in 1997 in favor of methods using newer instruments.  This method may still be useful to those laboratories that continue to operate packed column gas chromatographs.

END