U.S. CUSTOMS AND BORDER

PROTECTION LABORATORY METHODS

CBPL METHOD 38-09

ASTM D 3465

Standard Test Method for Purity of Monomeric

Plasticizers by Gas Chromatography

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

The following reference contains a packed column gas chromatographic procedure for determining the purity of monomeric plasticizers.  This method is limited to monomeric plasticizers with definite boiling points.  Many monomeric plasticizers may have boiling points exceeding 400 °C. Their determination depends on the availability of maximum column temperatures exceeding 300 °C.  Mixtures of monomeric plasticizers are provided for in Chapter 38, Heading 3812, of the Harmonized Tariff Schedule of the United States (HTSUS).

1.		REFERENCE

1.1		ASTM D 3465.  “Standard Test Method for Purity of Monomeric Plasticizers by Gas Chromatography.”

END