U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 39-30

USP/NF <731>

Loss on Drying

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

The procedure outlines general instructions for determining non-volatile/volatile material in a sample.  Normally, oven temperature is 105 °C (±5 °C).

This procedure is used for samples (other than collodions) consisting of any of the products of volatile organic solvent when the weight of the solvent is less than 50 percent of the weight of the solution.

These goods are provided for in Chapter 39 of the Harmonized Tariff Schedule of the United States (HTSUS), Headings 3901 to 3913.

1.		REFERENCE

1.1		USP/NF <731>.  “Loss on Drying.”

END