U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 50-25

NHM

ISO/TR 5090

Textiles—Methods for the Removal of Non-fibrous

Matter Prior to Quantitative Analysis of Fibre Mixtures

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF					APPLICATION

This method addresses the chemical removal of non-fibrous matter from textile commodities.  The method is suitable for analysis of goods provided for in Chapter 50 of the Harmonized Tariff Schedule of the United States (HTSUS).

1.		REFERENCE

1.1		ISO/TR 5090.  “Textiles—Methods for the Removal of Non-fibrous Matter Prior to Quantitative Analysis of Fibre Mixtures.”

END