U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 51-09

NHM

ASTM D 2260

Standard Tables of Conversion Factors and Equivalent

Yarn Numbers Measured in Various Numbering Systems

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

This method may be applicable to commodities classifiable in Chapter 51 of the Harmonized Tariff Schedule of the United States (HTSUS).  The reference consists of tables including (1) a series of conversion factors required to convert the number of a yarn measured in a specific system to the equivalent number measured in various other systems, and (2) specific equivalent numbers of yarns measured in various systems.  Yarn number information on invoices, therefore, could be converted into that specific system being used to classify a commodity in the HTSUS.

1.		REFERENCE

1.1		ASTM D 2260.  “Standard Tables of Conversion Factors and Equivalent Yarn Numbers Measured in Various Numbering Systems.”

END