U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 51-13

ASTM D 4157

Standard Test Method for Abrasion Resistance of

Textile Fabrics (Oscillatory Cylinder Method)

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

This reference covers the determination of the abrasion resistance of woven textile fabrics using the oscillatory cylinder tester.  The method may not be suitable for some fabric constructions. This may be applicable in evaluating upholstery fabrics classifiable in Chapter 51 of the Harmonized Tariff Schedule of the United States (HTSUS).

1.		REFERENCE

1.1		ASTM D 4157.  “Standard Test Method for Abrasion Resistance of Textile Fabrics (Oscillatory Cylinder Method).”

END