U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 54-02

NHM

# ASTM D 2256

##### Standard Test Method for Tensile Properties

##### of Yarns by the Single-Strand Method

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

This method covers the tensile properties of yarns.  It is suitable for the determination of high tenacity of man-made filament yarn and fabrics in Chapter 54 of the Harmonized Tariff Schedule of the United States (HTSUS).

Use of this method to address quantitative HTSUS criteria requiring specified accuracy should include a determination of the precision and accuracy and an evaluation of its fitness for use in the specific application.

1.		REFERENCE

1.1		ASTM D 2256.  “Standard Test Method for Tensile Properties of Yarns by the Single-Strand Method.”

END