U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 25-05

NHM

ASTM C 561

Standard Test Method for Ash in a Graphite Sample

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		INTRODUCTION

This method provides a quick and practical means of determining the ash content of graphite.  It is usually run consecutively with 2.2.  The method is widely used to determine the ash content of most carbon products.

1.		SCOPE AND FIELD OF 					APPLICATION

This method may prove useful in the analysis of commodities provided for in Chapter 25 of the Harmonized Tariff Schedule of the United States (HTSUS).  The ash content of graphite is the primary determinant of the purity of the sample.  High purity is normally associated with artificially produced graphite of HTSUS 3801.

2.		REFERENCE

2.1		ASTM C 561.  “Standard Test Method for Ash in a Graphite Sample.”

2.2		ASTM C 562, “Standard Test Method for Moisture in a Graphite Sample.”

END