U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 25-21

ASTM D 2131

Standard Classification for Natural Muscovite Mica Splittings

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

This specification provides a classification system of thirteen grades based upon size, form, and splittings thickness.  The grades are then qualified by meeting minimum defects requirements as determined by a counting method.  This method appears to be an attempt to classify mica splittings provided for in Chapter 25, Subheading 2525.10, of the Harmonized Tariff Schedule of the United States (HTSUS) and is an organized, less subjective system than the Bengal Indian System.

1.		REFERENCE

###### 1.1		ASTM D 2131.  “Standard Classification for Natural Muscovite Mica Splittings.”

END