U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 26-04

ASTM E 342

Standard Test Method for Determination of Chromium Oxide

in Chrome Ores by Permanganate Titrimetry

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

This method covers the determination of chromium oxide in chrome ores in the concentration range from 25 to 60 percent.  This method is suitable for the analysis of chromic oxide provided for in Chapter 26 of the Harmonized Tariff Schedule of the United States (HTSUS).

1.		REFERENCE

## 1.1		ASTM E 342.  “Standard Test Method for Determination of Chromium Oxide in Chrome Ores by Permanganate Titrimetry.”

END