U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 28-06

NHM

ASTM E 1371

Standard Test Method for Gravimetric Determination of

Phosphorus in Phosphorus-Copper Alloys or

Phosphorus-Copper-Silver Alloys

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

This method covers the gravimetric determination of phosphorus in phosphorus-copper or phosphorus-copper silver alloys containing 1 to 15 percent phosphorus.  The method may be useful in the analysis of commodities provided for in Chapter 28 of the Harmonized Tariff Schedule of the United States (HTSUS)

1.		REFERENCE

1.1		ASTM E 1371.  “Standard Test Method for Gravimetric Determination of Phosphorus in Phosphorus-Copper Alloys or Phosphorus-Copper-Silver Alloys.”

END