U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 44-09

TAPPI T 263

Identification of Wood and Fibers from Conifers

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

Wood products are provided for in Chapter 44 of the Harmonized Tariff Schedule of the United States (HTSUS).  TAPPI T 263 is the primary method for the identification of the species of wood.  If it is determined that the wood product is a softwood (section 7.1), this method is followed in its entirety.

If it is determined that the wood product is a hardwood (section 7.1), identification of the wood species is accomplished by using the references cited in TAPPI T 263 and in the following list.

1.		REFERENCES

This list is provided for general guidance and should not be considered exhaustive.  The user is expected to seek current references pertaining to this method.

1.1		Properties of Imported Tropical Wood.  USDA Forest Service Research Paper, FPL 125.  United States Department of Agriculture Forest Service.  Madison WI.  1970.

1.2		Hoadley, R.B.  Identifying Wood.  Tauton Press.  Newton, CT.  1990.

1.3		Ilic, J.  CSIRO Atlas of Hardwoods.  Crawford House with CSIRO.  East Melbourne, Australia.  1991.

1.4		Kribs, D.A.  Commercial Foreign Woods on the American Market.  Dover Publications.  New York.  1968.

1.5		Metcalfe, C.R. and L. Chalk.  Anatomy of Dicotyledons (Vol. I & II).  Oxford University Press.  London.  1972.

1.6		Miles, A.  Photomicrographs of World Wood.  Her Majesty’s Stationary Office.  London.  1978.

1.7		TAPPI T 263.  “Identification of Wood and Fibers from Conifers.”

1.8		Wheeler, E.A., Baas, P., and P.E. Gasson (Eds.).  IAWA List of Microscopic Features for Hardwood Identification.  IAWA Committee.  Leiden, The Netherlands.  1989.

END