U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 51-05

NHM

ASTM D 1113

Standard Test Method for Vegetable Matter and

Other Alkali-Insoluble Impurities in Scoured Wool

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

Wool and related commodities are provided for in Chapter 51 of the Harmonized Tariff Schedule of the United States (HTSUS).

The following reference contains procedures that should prove useful in determining the content of oven-dried, ash-free, alcohol extractive-free vegetable matter and other alkali-insoluble impurities present in scoured wool and related fibers, such as hair from goat, camel, alpaca, and similar animals.  This method aids in determining the extent of processing a wool or hair fiber has undergone in order to verify its HTSUS classification.

1.		REFERENCE

1.1		ASTM D 1113.  “Standard Test Method for Vegetable Matter and Other Alkali-Insoluble Impurities in Scoured Wool.”

END