U.S. CUSTOMS AND BORDER

PROTECTION LABORATORY METHODS

CBPL METHOD 51-18

NHM 006

Textiles—Methods and Procedures for the Analysis of Wool,

Fine or Coarse Animal Hair; Horsehair Yarn, and Woven Fabric

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

The methods and procedures described in this NAFTA Harmonized Method (NHM) address the identification of wool and animal hair fibers of various types.  This method may be applicable to the analysis of articles classified in Chapter 51 of the Harmonized Tariff Schedule of the United States (HTSUS).

1.		REFERENCE

1.1		NHM 006.  “Textiles—Methods and Procedures for the Analysis of Wool, Fine or Coarse Animal Hair; Horsehair Yarn, and Woven Fabric.”

END