U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 50-02

ASTM D 629

Standard Test Methods for

Quantitative Analysis of Textiles

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

## METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

The method specifies the determination of the quantities of textile fibers in blended materials by chemical, physical, and microscopic means.  It also details requirements for accounting for nonfibrous materials in both greige and converted fabrics (yarns).  This method is suitable the commodities of the Harmonized Tariff Schedule of the United States (HTSUS) Chapter 50.

1.		REFERENCES

1.1		ASTM D 629, "Standard Test Methods for Quantitative Analysis of Textiles."

1.2		Explanatory Notes to the Harmonized Commodity Description and Coding System, Vol. 2.  Section XI, General (I) (a) (5).

1.3		Parker, M.J.  "Analysis of Mixed Textile Materials Containing Sizing or Dressings.”  Customs Laboratory Bulletin.  4:4.  April 1992.

2.		REMOVAL OF NONFIBROUS 			MATERIALS

2.1		Greige Fabrics (Yarns):  Provisions in Reference 1.2 stipulate that "sizings or dressings (e.g., weighting (loading) in the case of silk) . . . incorporated in textile fibers are not deemed to be non-textile materials; [that] the weight of the textile fibers is calculated on the basis of their weight in the state in which they are presented."

2.2		Converted Fabrics (Yarns):  Provisions in Reference 1.2 stipulate that "sizings or dressings (e.g., weighting (loading) in the case of silk) . . . incorporated in textile fibers are not deemed to be non-textile materials; [that] the weight of the textile fibers is calculated on the basis of their weight in the state in which they are presented."

2.3		See References 1.1, Section titled “Nonfibrous Materials,” and 1.3 for additional information pertaining to both greige and converted fabrics (yarns).

END