U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 50-23

NHM

ISO 139

Textiles—Standard Atmospheres for Conditioning and Testing

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF APPLICATION

This method sets forth specifications for a standard temperature and atmosphere.  All items in Section XI of the Harmonized Tariff Schedule of the United States (HTSUS) are subject to testing under these conditions.

The standard temperate atmosphere for textile testing is: Relative Humidity (RH) of 65 percent (%) +/- 2 % and Temperature 20 degrees Celsius (ºC), +/- 2 ºC.

1.		REFERENCE

1.1		ISO 139.  “Textiles–Standard Atmospheres for Conditioning and Testing.”

END