U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 51-06

NHM

# ASTM D 2130

# Standard Test Method for Diameter of Wool

# and Other Animal Fibers by Microprojection

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

# Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

# METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

0.		SCOPE AND FIELD OF 					APPLICATION

The following reference contains procedures, using a microprojector, that are useful for the determination of the average fiber diameter and the fiber diameter variation of wool and other fine animal fibers such as mohair, cashmere, alpaca, camel hair, etc. in their various forms.  These products are classified in Chapter 51 of the Harmonized Tariff Schedule of the United States (HTSUS).

1.		SPECIAL CASES

The laboratory may use image analysis systems as a screening technique as follows:

1.1		Image analysis screening finds that the sample is not dutiable.  The sample is reported as such without further analysis.

1.2		Image analysis screening confirms an importer’s claim of grade, whether dutiable or not.  The sample is so reported without further analysis.

1.3		If, however, image analysis screening contradicts an importer’s claim of grade, or when no importer’s information is received and the sample is found to be dutiable, then the grade must be determined by the referenced microprojector method, ASTM D 2130.

## 2.		REFERENCES

This list is provided for general guidance and should not be considered exhaustive.  The user is expected to seek current references pertaining to this method.

2.1		ASTM D 2130.  “Standard Test Method for Diameter of Wool and Other Animal Fibers by Microprojection.”

2.2		ASTM D 3510.  “Standard Test Method for Diameter of Wool and Other Animal Fibers by Image Analyzer.”  ”[Discontinued 1987.  See 1986 Annual Book of ASTM Standards, Vol. 07.02, p. 666.]

2.3		Luniak, Bruno.  The Identification of Textile Fibres.  Sir Isaac Pitman & Sons, Ltd.  London.  1953.

2.4		Wildman, A.B.  The Microscopy of Animal Textile Fibres.  Wool Industries Research Association.  Leeds (UK).  1954.

### END