- U.S. CUSTOMS LABORATORY METHODS

- USCL METHOD 69-02

- (Date 11/19/99)

- Procedures for Measuring the Whiteness of Ceramic Products

ASTM Standards for Determining the Color of Objects by Visual or Instrumental Means and Specifying It by the Munsell Color System

# SAFETY PRECAUTIONS

This method does not purport to address all of the safety problems, if any, associated with its use.  It is the responsibility of the user of this method to establish appropriate safety and health practices and determine the applicability of regulatory limitations prior to its use.

- 1	SCOPE AND FIELD OF APPLICATION

- 1.1	General

1.1.1	The method employs the Munsell 	Color System, a widely used system 	of specifying color based on color 	perception attributes of hue, value, 	and chroma.  It is used to determine 	whether the bodies of non-artificially 	colored ceramic ware meet the 	"white" characteristic, as stated in 	the Explanatory Notes to Chapter 	69, of the Harmonized Tariff 		Schedules (HTS).  Ceramic ware are 	usually classifiable under HTS 	headings 6909, 6910, 6911, 6913 	and 6914.  The measurements may 	be performed visually or with an 	instrument.

    - Non-artificially colored sanitary ware

having a Munsell color of N 8.5 or                 lighter (in a neutral color shade 	having a chroma of 0 to 0.5) meets               the “white “ characteristic of the                     porcelain definition.

  - U.S. Requirements

1.2.1	Where necessary, the Additional 	U.S. Notes to Chapter 69, 		Harmonized Tariff Schedules of the 	United States (HTSUS), and various 	U.S. Customs Headquarters Rulings 	shall be followed.

1.2.2    For ceramic sanitary ware, see 	Federal Register, 61, 9521 (1996), 	as well as U.S. Customs 	Headquarters rulings HQ 958647 	and HQ 957520.

- 2	REFERENCES

- ASTM D 1535

Practice for Specifying Color by the Munsell System

- ASTM E 1164

Practice for Obtaining 		Spectrophotometric Data for Object-	Color Evaluation

ASTM E 1331

Test Method for Reflectance Factor 	and Color by Spectrophotometry 	Using Hemispherical Geometry

ASTM E 1347

Test Method for Color and Color-	Difference Measurement by 		Tristimulus (Filter) Colorimetry

ASTM E 1348

Test Method for Transmittance and 	Color by Spectrophotometry Using 	Hemispherical Geometry

ASTM E 1349

Test Method for Reflectance Factor 	and Color by Spectrophotometry 	Using Bidirectional Geometry

End of Method