U.S. CUSTOMS AND BORDER PROTECTION

LABORATORY METHODS

CBPL METHOD 73-23

Recommended Guidelines for the

Identification of Polymeric Materials

SAFETY STATEMENT

This CBPL Method cannot fully address safety issues that may arise from its use.  The analyst is responsible for assessing potential safety issues associated with a given method at its point of use.

Before using this method, the analyst will consider all general laboratory safety precautions.  In particular, the analyst will identify and implement suitable health and safety measures and will comply with all pertinent regulations.

METHOD UNCERTAINTY

The uncertainty of measurement for this method is specific to each laboratory.

# 0.		SCOPE AND FIELD OF 					APPLICATION

These guidelines are intended to aid in the identification of polymeric materials used as coatings on articles of iron or steel in Chapter 73 of the Harmonized Tariff Schedule of the United States (HTSUS).

# 1.		REFERENCES

## This list is provided for general guidance and should not be considered exhaustive.  The user is expected to seek current references pertaining to this method.

## 1.1		Bibawy, N. A.  “Preparation of Polymer Samples for Qualitative Analysis” in Customs Laboratory Bulletin.  6(4).  Pp. 187-207.  1994.

## 1.2		Brezinski, D.R. (Editor).  An Infrared Spectroscopy Atlas for the Coatings Industry.  Federation of Societies for Coating Technology.  Blue Bell, PA.  1991.

## 1.3		Byington, J.I., Mohl, D., and Chan, E.  “Analysis of Plastic Sheeting by FT-IR Microscopy” in Customs Laboratory Bulletin.  6(2).  Pp. 115-123.  1994.

## 1.4		Crompton, T.R.  Analysis of Polymers: An Introduction.  Pergamon Press.  Oxford.  1989.

## 1.5		Farber, Leon.  “Polymer Types and Structures” in Customs Laboratory Bulletin.  6(2) 53-84.  1994.

## 1.6		Harris, R.  “Qualitative Identification Tests for Plastics” in Customs Laboratory Bulletin.  6(4) 209-225.  1994.

## 1.7		Haslam, J., Willis, H.A., and Squirrell, D.C.M.  Identification and Analysis of Plastics, Second Edition.  Butterworths.  London.  1972.

## 1.8		Hummel, D.O. and Scholl, F.  Atlas of Polymer and Plastics Analysis, Second Edition.  Hanser.  Munich.  1981.

## 1.9		Krause, A., Lange, A., and Ezrin, M.  Plastics Analysis Guide: Chemical and Instrumental Analysis.  Hanser.  Munich.  1983.

## 1.10		Lucchesi, C.A. and McGuinness, J.D.  “Methods for the Analysis of Plastic Resins” in Handbook of Analytical Chemistry.  L. Meites (Editor).  McGraw-Hill.  New York.  Pp. 13-210 to 13-226.  1963.

## 1.11		Mark, H.F., Bikales, N.M., Overberger, C.G., Menges, B., and Kroschwitz, J.I. (Editors).  Encyclopedia of Polymer Science and Technology, Second Edition.  John Wiley and Sons.  New York.  1990.

## 1.12		Roff, W.J., Scott J.R., and Pacitti, J.  Handbook of Common Polymers.  CRC Press.  Cleveland.  1991.

END